THE INTERNATIONAL GROUP, INC.

85 Old Eagle School Road · P.O. Box 384 · Wayne, PA 19087· (610) 687-9030 · Fax (610) 254-8548

50 Salome Drive · Agincourt, Ontario, Canada M1S 2A8 · (416) 293-4151 · Fax (416) 293-0344

PARAFFLEX® 4630A

PARAFFLEX® 4630A is a soft, smooth and creamy looking blend specially formulated

for single pour container candles.

PHYSICAL PROPERTIES

ASTM		SPECIFICATIONS

TEST METHODS  			METHOD 	Minimum 	Maximum 	TYPICAL

Congealing Point °F (°C): zb		D 938 		115 (46.1) 	125 (51.7) 	120 (48.9)

Kinematic Viscosity cSt@212°F (100°C) D 445 		5.0 		6.5 		5.7

Saybolt Color zo			D 6045 	+8 		---- 		+13

Odor zq					D 1833 	---- 		1 		0.5

Needle Penetration, dmm@77°F (25°C)	D 1321 	95 		135 		125

Note: Physical properties for which ONLY a typical value is listed are included as additional information but may not be printed on the COA.

FDA STATUS:

Please contact an IGI representative for information concerning the FDA status of this product.

4600\4630A

WARRANTY DISCLAIMER STATEMENT

The information contained in this bulletin is based on tests which are believed to be reliable. As actual conditions of use may vary and are beyond the control of THE

INTERNATIONAL GROUP, INC. the product’s specified characteristics cannot be guaranteed and are offered solely for the buyers evaluation and verification. There are no

warranties, representations or conditions, expressed or implied, of any kind, including, but limited to, merchantability or fitness for a particular purpose made by THE

INTERNATIONAL GROUP, INC. or its officers, employees or affiliates, in connection with the sale of the products described in this bulletin. Accordingly, the purchaser and

each user assumes all risks and liability in connection with their use of such products. Nothing contained herein is to be construed as permission, recommendation or

inducement by THE INTERNATIONAL GROUP, INC. or its officers, employees or affiliates, to use any product or process so as to infringe or conflict with any patent. Further,

it is the user’s obligation to utilize this material in full compliance with health, safety and environmental regulations. THE INTERNATIONAL GROUP, INC. recommends that the

Material Safety Data Sheet for this product be consulted prior to handling.