THE INTERNATIONAL GROUP, INC.

85 Old Eagle School Road · P.O. Box 384 · Wayne, PA 19087· (610) 687-9030 · Fax (610) 254-8548

50 Salome Drive · Agincourt, Ontario, Canada M1S 2A8 · (416) 293-4151 · Fax (416) 293-0344

.

Product Information Sheet 4633A (ASTORLITE® J223)

Product Description

A soft, smooth and creamy looking blend designed for manufacturing container candles

Typical Properties Congealing Point: (ASTM D938): 128°F (53.3°C)

Needle Penetration: (ASTM D1321 @77°F): 108 dmm

Appearance (solid):

Benefits Parafflex 4633A is a fairly soft, smooth, white to off-white, creamy and opaque blend

designed for manufacturing container candles.

Guidelines

• A soft, cloudy, creamy looking multiple pour container candle wax.

• Can accommodate fragrance oil up to a 10% level with no bleed.

• Exhibits good adhesion to glass containers when poured under the specified

conditions.

• Good burn characteristics when used with a wick of appropriate size.

• Available in fiber drums and bulk.

• Container pre-warming: Containers should be pre-warmed to at least 130°F (55°C).

• Pour Temperature: 175 - 200°F (79 - 94°C).

• Fragrances and dyes specifically developed for candles should be used.

Packaging, Product Form, and Storage Conditions

Solid product should be stored at ambient room temperature in a clean, dry environment

with the original packing. Bulk liquid product should use dedicated tanks and lines. Please

contact IGI representative for additional storage details or alternate packaging forms.

THE INTERNATIONAL GROUP, INC.

85 Old Eagle School Road · P.O. Box 384 · Wayne, PA 19087· (610) 687-9030 · Fax (610) 254-8548

50 Salome Drive · Agincourt, Ontario, Canada M1S 2A8 · (416) 293-4151 · Fax (416) 293-0344

4600\4633A

Certificate of Analysis

IGI 4633A (ASTORLITE® J223) is a soft, smooth, creamy looking container candle formulation

designed specifically to enhance both hot and cold fragrance throw. The wax performs

best when poured at 145 - 155°F into a heated container.

PHYSICAL PROPERTIES

ASTM		SPECIFICATIONS

TEST METHODS 			METHOD 	Minimum 	Maximum 	TYPICAL

Congealing Point °F (°C) zb		D 938 		117 (47.2) 	128 (53.3) 	124 (51.1)

Kinematic Viscosity, cSt @ 212°F (100°C) zdD 445 		5.0 		6.5 		5.7

Saybolt Color zo			D 6045 	+8 		---- 		----

Odor zq					D 1833 	---- 		1.0 		0.5

Needle Penetration, dmm @77°F (25°C)	D 1321 	95 		135 		108

Note: Physical properties for which ONLY a typical value is listed are included as additional information but may not be printed on the COA.

FDA STATUS:

This product meets the FDA requirements set forth in 21 CFR 178.3710 for use in nonfood

articles in contact with food and in 21 CFR 172.886 for use in food.